## Slide 1
Ion irradiation effects in plasma-facing tungsten and its potential alloys
Prof. Enrique Jimenez-Melero
UKAEA Joint Chair in Materials for Fusion
School of Metallurgy and Materials
University of Birmingham
e.jimenez-melero@bham.ac.uk
Presentation at Third DONES Users Workshop
Tuesday 2nd October 2024, 15:45-16:00h
Zagreb (Croatia)

## Slide 2
Composition change due to 14 MeV neutron
irradiation of W (wall loading of 2 MW m-2)
Transmutations & alloy strategies in W
I. Ipatova, E. Jimenez-Melero et al., J. Nucl. Mater. 501 (2018) 329-335
G.A. Cottrell, J. Nucl. Mater. 334 (2004) 166-168
D. Hancock, J. Nucl. Mater. 512 (2018) 169-183

## Slide 3
Can Ta alloying in W influence low-energy/high-fluence He bubble formation?
Single ITER divertor
cassette
G. De Temmerman, Plasma Phys. Control. Fusion 60 (2018) 044018
30 eV He plasma exposures
at  400 °C
He energies: eV regime
DIFFER
(Netherlands)

## Slide 4
Can Ta alloying in W influence low-energy/high-fluence He bubble formation?
E. Yildirim, E. Jimenez-Melero, Fusion Eng. Des. 197 (2023) 114061
Surface
He fluence 1027 m-2

## Slide 5
He bubble formation at 800 °C
Unalloyed W
I. Ipatova, E. Jimenez-Melero, J. Nucl. Mater. 550 (2021) 152910
He energies: keV regime

## Slide 6
W-5Ta
I. Ipatova, E. Jimenez-Melero, J. Nucl. Mater. 550 (2021) 152910
He bubble formation at 800 °C

## Slide 7
Mechanism of He bubble formation
Interstitial He atoms are mobile (Em = 0.06 eV) and aggregate to form clusters
Self-trapping mechanism: x Hei + Hei  (x+1) He-vac + SIA
Trap mutation mechanism: x He-vac + Hei  (x+1) He-2vac + SIA
E (Hei-Hei) = 1.03 eV (1.64 eV for a 4Hei cluster)
E (Hei-vac) = 4.57 eV (decreases with a higher He/vac ratio in the cluster)
E (Hei-SIA) = 0.94 eV  He de-trapped from SIAs are trapped by vacs
SIAs are mobile below RT, whereas single vacs start to be mobile at T  200-300 °C
He-vac clusters present significant mobility at T  600 °C  growth by cluster coalescence

## Slide 8
Dual beam irradiations in tungsten at 800 °C
In-situ TEM under dual irradiations
300 kV Hitachi H-9500 TEM
(Univ. Huddersfield, UK)
Experiment | Composition | Temp. (°C) | Time (s) | Flux | Damage (dpa) | Ion Energy
W+He (concurrent) | W | 800 | 800 |  | 0.2(W)+ 0.3(He) | 600 keV (W2+) 10 keV (He+)
W+He (sequential) | W | 800 | 800+660 |  | 0.2(W)+ 0.3(He) | 600 keV (W2+) 10 keV (He+)
Experiment | Composition | Temp. (°C) | Time (s) |  | Damage (dpa) | Ion Energy
W+He (concurrent) | W | 800 | 800 |  | 0.2(W)+ 0.3(He) | 600 keV (W2+) 10 keV (He+)
W+He (sequential) | W | 800 | 800+660 |  | 0.2(W)+ 0.3(He) | 600 keV (W2+) 10 keV (He+)
10 keV He+
600 keV W2+
E. Yildirim, E. Jimenez-Melero, Nucl. Mater. Energy 39 (2024) 101672

## Slide 9
Dual beam irradiations in tungsten at 800 °C

## Slide 10
‘Post-mortem’ characterizations
of irradiated tungsten
Sample | Time (s) | Flux (m-2 s-1) | Damage (dpa) | Ion energy (keV) | Void diameter (nm) | Bubble density (m-2)
WSQN | 800 660 | 7 × 1014 2 × 1017 | 0.2 0.3 | 600 W2+ 10 He+ | 2.0 ± 0.6 | 6.7 ± 0.6
WCON | 800 | 7 × 1014 1.7 × 1017 | 0.5 | 600 W2+ 10 He+ | 1.7 ± 0.5 | 11.1 ± 0.7

## Slide 11
Beam line development – radiation damage to materials
P. Wady, E. Jimenez-Melero, Nucl. Inst. Meth. Phys. Res. B 806 (2016) 109

## Slide 12
Motorized slit system
Beam alignment
Define the sample
irradiated area
Independent current
integration
Sample stages
P. Wady, E. Jimenez-Melero et al., Accelerated radiation damage test facility using a 5MV
tandem ion accelerator, NIMPRB 806 (2016) 109-116
a
b

## Slide 13
W
W-5Ta
3MeV Proton irradiations
T = 350 C
Proton energies: MeV regime

## Slide 14
W-base alloys as plasma
facing materials
I. Ipatova, E. Jimenez-Melero et al., J. Nucl. Mater. 501 (2018) 329-335
(40 keV)
(3 MeV)

## Slide 15
Fusion Steels (0.5mm thick)
1. coupons (thermal testing)
2. dog-bone SSJ2 specimens
Proton energies: 3-38 MeV
Tirr  500 C
3 MeV H  35 µm
10 MeV H  257 µm
28 MeV H   1.5 mm
Irradiated area: 1 cm2
MC40 cyclotron
Proton Irradiations
Neutron irradiations
Li(p,n) source (possibly also d,n)
2.6 MeV p -> neutrons < 0.9MeV