## Slide 1: IFMIF-DONES Lithium Systems
J. Maestre
9th Annual RaDIATE Collaboration Meeting. 16-18 Sept. Granada (Spain)

## Slide 2: Outline
Validations and prototyping
Target System
Conclusions
Overview to Lithium systems

## Slide 3: Lithium System: introduction
Lithiujm system
15
A neutron flux of ~ 1018 – 1019 n m2/s
is generated with a neutron spectrum up to 55 MeV energy.

## Slide 4: Lithium System: introduction
R015
Oil Loop Cell
R016 Lithium Loop Cell
R009-1
Cold trap
R009-2
H-trap
BEAM
Liquid lithium Target

## Slide 5: Lithium Systems
Generating a stable liquid lithium target for enabling D-Li stripping reaction and producing an adequate neutron flux to properly irradiate the test modules downstream.
Systems:
Target System: To provide a continuous Li jet whose interaction with D+ beam generates the Neutron flux.
Heat Removal Loop: To remove the energy deposition on the Lithium.
Impurity Control System: To localize and control the impurities in the Lithium.

## Slide 6: Heat Removal Loop
The system consists of:
Primary Lithium Loop (PLO)
Tertiary Oil Loop
(TLO)
Secondary Oil Loop (SLO)
Water rejection system
Main parameters:
Li inventory ~14 m3
Li flow rate ~100 l/s
Li working temperature (cold side) 300 °C
Deposited power: 5 - 10 MW

## Slide 7: Heat Removal Loop: EMP
Main parameters:
Design temp: 350 ºC
Flow rate: 100 l/s
Discharged pressure: 4 bars
Challenge:
Extreme low NPSH (Net Positive Suction Head) < 1 bar
Flywheel concept
Inlet
Pressure increase

## Slide 8: Impurity Control System
To control and confine the sources of radioactivity such as tritium (T), beryllium-7 (Be-7) and activated corrosion products (ACP), i.e. corroded/eroded metallic elements .
To control and capture the sources of the corrosion and erosion on structural components such as oxygen (O), carbon (C), hydrogen (H) and nitrogen (N).
To monitor the impurities in the liquid lithium and to assure the optimal physical conditions.
Functions:
To control and confine the sources of radioactivity such as tritium (T), beryllium-7 (Be-7) and activated corrosion products (ACP), i.e. corroded/eroded metallic elements .
To control and capture the sources of the corrosion and erosion on structural components such as oxygen (O), carbon (C), hydrogen (H) and nitrogen (N).
To monitor the impurities in the liquid lithium and to assure the optimal physical conditions.
Test of structural stainless stell alloys on static liquid lithium [1]
[1] S.k. Parida et al. Studies on chemical compatibility of steels with liquid lithium. Journal of Nuclear Materials 526 (2019) 151761
[2] X.C. Meng et al. Corrosion characteristics of copper in static liquid lithium under high vacuum. Journal of Nuclear Materials, Volume 513, January 2019
Clear attack to grain and also to grain boundary (see 316L)
Temperature dependent
Impurity dependent (N, O, H)
Static test of Cooper with Liquid lithium at 620 K for 15 h under high vacuum [2]

## Slide 9: Impurity Control System
Corrosion Products (CP) are generated continuously due to the contact between the liquid
T and 7Be are produced as results of the nuclear interaction Li-Deuteron beam.
N, O and C may be incorporated due to maintenance or replacement of Li equipment.
Cold traps: To remove soluble compounds with temperature dependent solubility by crystallization on a wire mesh substrate. The processes are film driven after initial crystallization. Mainly focused of Li with O, H and C; but also for CPs and ACPs, including 7Be compounds.
Hydrogen traps: To remove the H isotopes by a gettering process similar to the N-trap. Yttrium (Y) has been selected as a suitable getter material. Trap working online.
Nitrogen trap: To remove the Nitrogen from the liquid lithium. The process is driven by mass transfer in the liquid lithium and subsequent N capture and diffusion inside the getter. The trap operates offline on the whole Lithium inventory
Sources

## Slide 10: Impurity Control System
LIFUS 6 (ENEA Brasimone). Facility devoted to corrosion and erosion tests of structural material under flowing lithium.
ANGEL facility. (ENEA Brasimone). Facility aiming at investigating getters materials for N trapping in Liquid Lithium at lab scale.
Lyder. (CIEMAT-Madrid). Facility aiming at investigating H-getter in liquid lithium at lab scale.
LITEC (CIEMAT-Granada). Facility aiming at investigating purification and monitoring technologies a full DONES scale under representative conditions

## Slide 11: Target System: description
Beam
Target is allocated inside Test Cell, concrete cell covered by a stainless-steel liner.
TC shall provide enough shielding to adjacent rooms
TC provides the proper working conditions and boundaries (to the target and experimental modules), controlling the environment (low pressure He or Ar)
Temperature of the liner controlled by water cooling system on the outside
10 m

## Slide 12: Target System: description
Nominal liquid Lithium jet speed of 15 m/s at the exit of the nozzle (but up to 20 m/s in case of IFMIF)
Curvature of BP for avoiding Li boiling
25 mm thin Li jet and slim Back Plate to reduce neutron re-absorption (1.8 mm thickness)
Inlet nozzle
10E-4 mbar
Through wall beam duct
Function
Receive the beam (200 x 50 or 100 x 50 m2) and deliver the neutron flux
BackPlate
Inlet nozzle
BEAM

## Slide 13: Target System: analysis
High density power deposition in the Li jet ~85 kW/cm3
Deuterium Bragg - Peak at 20 mm (25±1 mm thickness)
Distribution of power deposition also in the rest of the Target structure due to neutron and photons (~1 W/cm3)
P= 10E-4 mbar
Fig. Beam energy deposition on the lithium jet
Courtesy of S. Gordeev, A. Serikov, Q. Yuefeng (KIT, Germany)
Fig. Heat power deposition on the structure
200 mm (100)
50 mm

## Slide 14: Target System: analysis
High temperature localized in the bulk lithium (~425ºC for nominal beam size), whilst at the free surface is in rather low ~325ºC
QT homogenizes the temperature (318 ºC) and quenches the flowing lithium before being reinjected to the Li loop
Suitable design of the Back plate to prevent boiling at the free surface and inside Li jet.
Fig. Temp distribution in the Li jet and Quench Tank during beam on
Nominal beam size 200 x 50 mm2
Q = 97.5 L/s
Tin = 300ºC
BEAM
P [Pa]
Y
- VLi 20 m/s
Variable curvature
P= 10E-2 Pa
Pressure distribution in the Li jet
10E-4 mbar
Chart: Vapour pressure of Lithium
- VLi 20 m/s
- VLi 15 m/s
- VLi 10 m/s
Margin in temp.
Margin in pressure
BEAM

## Slide 15: Target System: Material
Eurofer-97
AISI 316L
Nominal Wolking temperatura 300-320ºC
Nominal Wolking temperatura 50-150ºC
 | EUROFER-97 (Ferritic-martensitic) | ANSI 316L(N) (Austenitic)
Activation | Low activation stainless steel (fewer long-lived radioactive isotopes) | -
Mech. Prop: temperature | Good mechanical properties at elevated temperatures (<550 °C), suitable thermal conductivity and fatigue behavior (when comparing with other stainless steel). | Acceptable properties at high temperature (<550 )
Mech. Prop: creep/swelling | Lower swelling/creep at high temp (>400 ºC) under irradiation. | Prone to swelling (>400 °C), though negligible a lower temperatures
Mech. Prop: irradiation hardening/ embrittlement | Significant irradiation hardening especially at "low" temperatures (< 300 °C) | Significant embrittlement in the range of 300-350 °C
Corrosion resistance | Good resistance to corrosion and erosion under liquid metals | Acceptable resistance to corrosion and erosion under liquid metals
Other | no qualified | Qualified for nuclear applications (fission) up to 53 dpa
EUROFER exhibits a shift on its behaviour from ductile to brittle for a given range of temperature, called DBTT. No irradiated one is about ~ -90 °C, so it is not an issue for normal applications.
When the material is irradiated with high energy neutrons, the DBTT increases and, at high doses, it can eventually reach the operating temperature
Lifetime of Target ~ 8 months (yearly replacemente)

## Slide 16: Target System: Bayonet concept (under validation)
The suitability of the tested gasket to work in lithium environment has been proven up to 5500 hours (i.e., about 7.5 months)
Issue on 1 of 5 the test rig at 7000 hours. After post test analysis, possible ingress air leading to oxidation, so test should be repeted
Testing campaing on Sealing
Bayonet concept
Only the BP is removed.
Based on on energized gaskets (Helicoflex).

## Slide 17: Target System: Irradiation samples
Simulations of expected DPA on the backplate for beam 200 x 50 mm2
Why to not used the BP for characterization of Eurofer-97?
Preliminary specimen distribution in the BP
The back-plate of the IFMIF-DONES target assembly is subjected to strong neutron irradiation
Temperature conditions are quite homogeneous and stable
BP is strongly activated, so dedicated Hot cells and tools required for machining samples

## Slide 18: Target System: replacement
Replacement conducted by Remote-Handling means due to high dose inside TC.
Tight space within the TC, with limited accessibility to the components.

## Slide 19: Target System: replacement
Replacement strategy and features
Small gearboxes, spindle/nut, slidings (ceramic/ceramic or steel/ceramic)
QDS
Ball joints, slides
Excentres
Small gearboxes
Spindle drives, slides
TX
TX
TY
TZ
TZ
TX
TY
FDS
Fiducials
Gearboxes, spindle/nut, flexible shafts (remain in the TC)
Guided Fast disconnection system
Linked with the HFTM
Remote handling compatible
Centering features
Quite complex operation!
It should be tested and validated

## Slide 20: Validations and prototyping
Prototype of QDS/FDS
Target Mock-up
Manufacturing of prototype for connection and disconnection mechanism (QDS) by remote control in IFMIF-DONES project
Manufacturing of prototype for connection of the fast disconnection system (FDS) of the Li inlet pipe
Analysis of the RH procedure of the TSY
Results of Target Pre-heating Test (EFDA_D_2NHGLF v1.0)
Heating jacket
Back Plate
Analysis of Pre-heating procedures

## Slide 21: Validations and prototyping (IFMIF-EVEDA)
Engineering validation for lithium target facility of the IFMIF under IFMIF/EVEDA project. Nuclear Materials and Energy, Vol 9, pag. 278-285 (2016)
Fig. Prototype of the Target
Fig. free jet taken with 2 s and 10 µs exposure time
Fig. ELTL facility in Japan
Lithium Test Loop (ELTL) at Oarai (Japan) during IFMIF/EVEDA
Lithium loop at real scale 1:1 for loop high and 1:2.6 for target width with respect to DONES.
Long time operation (>3800 h)
Fluid-Dynamic stability of the Li jet (1300 h). Suitable flatness of the free surface (non uniformity < 0.28 mm)
Li jet ranging from 10 - 20 m/s
Validations

## Slide 22: Summary
Most of design activities are to be concluded soon, though still running some specific activities aim at further definition level.
Currently mostly focused on engineering validation activities.
  Replacement strategy of the Target System and auxiliary sub-systems.
  Diagnostic.
  Lithium Purification technologies
  Removable concept of the Back Plate of the Target.

## Slide 23: Thanks Any advice or suggestion is welcome

## Slide 24: Introduction
ITER (800 m3)
ITER under construction in Cadarache (France). To demonstrate the scientific feasibility of fusion energy (500 MW of power from fusion energy with Q>10) no connected to the grid.
DEMO (~1000-3500 m3):
Being designed to operate continuously providing electricity to the grid (~2-4 GW), showing commercial nuclear fusion is technically feasible. Q>10, 2050
JET (80 m3)
JET started its operations in 1983. It was designed to study plasma behaviour in conditions close to those required for a fusion reactor. (16MW and Q<1 still)
MAGENETIC CONFINEMENT FUSION
1-3 dpa/lifetime
~20 dpa/year
Main challenge:
Materials capable of withstanding the thermal loads and irradiation effects that may occur on the chamber walls.
See https://www.euro-fusion.org/eurofusion/roadmap/
Engineering Standards

## Slide 25: Introduction
Granada (Escúzar)

## Slide 26: Lithium Systems: overview
Accelerator System
Test System
Lithium System