## Slide 1: Analysis of Li traps mechanics and kinetics

## Slide 2: SUMMARY
Context
Cold trap
Getter trap

## Slide 3: Context (1/2)
The control of impurities in lithium is essential for the safe operation of the plant. Various impurities have already been identified as well as their sources and implications.
Non-metallic impurities
nitrogen
oxygen
Hydrogen (different isotopes)
carbon
Metal impurities
corrosion and erosion of Eurofer 97
Corrosion and erosion of stainless steel
Li beam interaction
Beryllium7
Tritium
Activated corrosion product
Purification goals: Contain and locate sources of radioactivity, limit corrosion, ensure the physical properties of liquid lithium

## Slide 4: Context (2/2)
Purpse
The aim of this task is therefore to collect additional informations on traps and getters, based on previous CEA experiences on other liquid metal facilities such as sodium to adapt or extrapolate the technologies and compare the responses of the different types of traps in terms of :
Purification rate
Treatment capacity

## Slide 5: Cold Trap (1/2)
Nitrogen capture:
High solubilities at 200°C ,
We can obtain for 100 hours of operation at near-melting temperature of lithium, 965 to 675 ppm of N2
Hydrogen capture :
At 200°C the solubility is about 60 ppm. (At the same temperature, the concentration of hydrogen in sodium is only 1 ppm).
It is therefore not very interesting to implement it for hydrogen alone
Schematic diagram of Cold Trap by WESTON [46]

## Slide 6: Cold Trap (2/2)
Oxygen capture :
YONCQ [30], the cold trap technique at 200°C should make it possible to obtain concentrations of less than 10 ppm.
Experimental results of various authors, while their cold trap temperature is close to 180°C, never reach this value.
WESTON [44] ratio of oxygen contents doesn’t fall below 100 ppm at 250°C. WESTON explains those anomalies either by the incomplete crystallization of Li2O in the cold trap, or by the presence of other oxides more soluble than Li2O.
Carbon capture :
For 3500 hours of operation, 120 ppm at 450°C
The minimum measured content was 10 ppm at 250°C
Schematic diagram of Cold Trap by WESTON [46]

## Slide 7: Getter Trap (1/3)
Nitrogen capture :
Titanium :
    With titanium in the form of sheets or sponges at 816°C, HOFFMANN [39] achieves concentrations of less than 10 ppm.
Zirconium :
  WESTON [56] starts from a nitrogen level of 1 200 ppm after 500 h, rises to 2 500 ppm and then decreases to 700 ppm in 2 000 h. (Entire loop at 700 - 800 K and hot trap at 900 K). But zirconium does not allow you to go below 100 ppm.
hot traps (Ti, Zr) operate at temperatures above 530 °C on low-pollution circuits
Schematic diagram of hot trap by BAGNALL [47]

## Slide 8: Getter Trap (2/3)
Carbon Capture:
OENEN [53] used a titanium sponge hot trap at 650°C on the lithium loop. This trap allows it to decrease the carbon content from 108 ppm to 3.6 ppm.
Hydrogen Capture:
This is the most widely used process because it has been the subject of numerous studies for tritium trapping.
The material of the hot trap or getter must be insoluble in lithium and form a hydride with hydrogen that is more stable than LiH
Although the literature does not mention a very complete experiment with the capture of hydrogen by yttrium, it seems that this method can reduce the content to a few ppm.
Schematic diagram of hot trap by BAGNALL [47]

## Slide 9: Getter Trap (3/3)
Oxygen capture:
Tests by HOFFMAN [25] with titanium sheet at 816°C showed an increase of oxygen in lithium and purification of the titanium sheet.
In contrast, tests with yttrium chips at 816°C for 100 h yielded a content of less than 100 ppm.
Schematic diagram of hot trap by BAGNALL [47]

## Slide 10: Conclusion
 | Oxygen | Hydrogen | Carbon | Nitrogen
Cold Trap | 10 ppm at 250°C | 60 ppm at 200°C | 120 ppm at 450°C during 3500h 10 ppm at 250 °C | 1000 ppm at T during 100h
Getter Trap | Yttrium chips: <100 ppm at 816°C during 100 h Titanium: 80 ppm at 820°C during 100 h | A few ppm | Titanium sponge at 605°C: concentration decreased from 108 ppm to 3.6 ppm | Titanium sheet at 816°C: 10 ppm Zirconium at 627°C: 700 ppm during 2000 h
 | Oxygen | Hydrogen | Carbon | Nitrogen
Cold Trap | 10 ppm at 250°C | 60 ppm at 200°C | 120 ppm at 450°C during 3500h 10 ppm at 250 °C | 
Getter Trap | Yttrium chips: <100 ppm at 816°C during 100 h Titanium: 80 ppm at 820°C during 100 h | A few ppm | Titanium sponge at 605°C: concentration decreased from 108 ppm to 3.6 ppm | Titanium sheet at 816°C: 10 ppm Zirconium at 627°C: 700 ppm during 2000 h
Performance of purification processes as a function of impurities

## Slide 11: Thank you for your attention

## Slide 12: Reference
[1] J. DESREUMAUX - G. LAPLANCHE; ETUDE BIBLIOGRAPHIQUE SUR LES INTERACTIONS DU LITHIUM ET DE L'AZOTE REACTION - PURIFICATION – CONTRÔLE
[2] J. DESREUMAUX - G. LAPLANCHE; ETUDE BIBLIOGRAPHIQUE SUR LES INTERACTIONS DU LITHIUM ET DU CARBONE REACTION - PURIFICATION – CONTRÔLE
[3] J. DESREUMAUX - G. LAPLANCHE; ETUDE BIBLIOGRAPHIQUE SUR LES INTERACTIONS DU LITHIUM AVEC L’HYDROGENE REACTION- PURIFICATION – CONTRÔLE
[4] J. DESREUMAUX - G. LAPLANCHE; ETUDE BIBLIOGRAPHIQUE SUR LES INTERACTIONS DU LITHIUM ET DE L'OXYGENE REACTION- PURIFICATION – CONTROLE