## Slide 1: Lithium purification experiments at laboratory scale
S.J. Hendricks, J. Molla, D. Jiménez, J. Navas, J. Patiño, M. Sanchez-Arenillas

## Slide 2: The problem of hydrogen isotope accumulation in DONES
!
 | H-isotopes in Li [g/yr]
T | 3.9
D | 86.87
H | 2.63
Accumulation of H isotopes leads to an increase in corrosion in the pipe system!
Radioactive nature of generated tritium is a severe safety issue!
Collision of D+ beam with the liquid Li target causes:
Sketch of DONES main Li loop:
International Atomic Energy Agency, 2023
Nakamura, 2002
D+ ray

## Slide 3: Need for hydrogen isotope purification in DONES
Type equation here.
Requirement for DONES:
1st limit: Concentration of all H isotopes
2nd limit: Mass of tritium in the lithium:
3rd limit: Mass of tritium in the yttrium:
Hydrogen isotopes should be absorbed by a getter trap that contains a hydrogen absorbing metal like yttrium, uranium or ZrCo.
Yttrium metal forms the most stable metal-hydrides (YH2) and can take up to three hydrogen isotopes per yttrium atom.
Yttrium is chemically compatible with corrosive liquid lithium.
The solubility of hydrogen in yttrium is several orders of magnitude higher than the solubility of hydrogen in lithium.
Without purification: Tritium limit exceeded after 28 days!
Flow of H into Y getter until chemical equilibrium!
Nakamura, 2002
Sketch of DONES main Li loop:
D+ ray

## Slide 4: Motivation and objective of work
Objective: Experimentally studying hydrogen isotope capture by an yttrium pebble bed to help defining the design parameters for an hydrogen trap which shall be capable of keeping the tritium content in the DONES lithium system below imposed concentration limits!
Nakamura, 2002

## Slide 5: LYDER: Lithium experiment for Yttrium-based DEeuterium Retention
A new liquid lithium experiment is designed and constructed to perform D retention experiments.

## Slide 6: LYDER: Lithium experiment for Yttrium-based DEeuterium Retention

## Slide 7
Design of the LYDER heating system
The lithium system is heated by 13 resistant heating cables and 28 thermocouples.
Commissioning: Heating system tested to 350 C, Glove box cooling and purification system tested!
D2 injection system

## Slide 8
A LabVIEW program is created to control and monitor the heating and vacuum system of the LYDER experiment.
LYDER LabVIEW control program

## Slide 9
First experiment: Test Li motion & Li extraction without D
bypass
drain valve
level meters
LT
RT
Lithium insertion and melting:
Test of lithium movement:
Test of sample extraction system:
Increased pressure in LT by 50 mbar and opened bypass valve to pump Li into RT.
By continuously injecting gas into LT the 50 mbar was maintained while Li surface rose in RT.
After 1 min level sensor circuits closed and pressure increase in LT showed disruptions signaling that all Li has arrived in RT.
Then, Li was pumped back to LT through the deuterium trap.
Filled LT with 100 mL of lithium pallets, evacuated, and injected 200 mbar overpressure of Ar into Li system before heating to
2mL of Li was extracted in sampler and dropped on a steel plate in the glove box

## Slide 10
The LYDER deuterium trap based on an yttrium bed
An yttrium-based D-trap is designed, manufactured and installed into the LYDER system.

## Slide 11
Experimental progress after first experiment
1.
2.
3.
4.
5.
6.
Removal of H trap container
Proof of Li flow through trap
Cleaning of trap in water
5g of yttrium pieces selected
Insertion of yttrium into trap
Mounting of Y-filled trap in LYDER
5 mm

## Slide 12: Design of the LYDER deuterium injection system
The deuterium injection system has been manufactured and installed at the bottom of the right tank.
Li level sensor I:
90 mL of Li has entered
D injection
system
Li level sensor II: Fe tube covered
Right tank
Argon gas inlet/outlet
Custom modified 40CF flange
Fabricated 0.5 mm thick Fe tube
Lithium inlet
View from above into right tank
D2 gas inlet
Li inlet

## Slide 13: Numerical model of the LYDER deuterium injection system
Injection method: Permeation of deuterium from gas chamber through a hollow α-Fe tube into liquid lithium!
The deuterium injection system for liquid Li is designed based on a developed model with EcosimPro©.
A similar design could be employed in future liquid lithium research loops to inject hydrogen impurities (e.g., LITEC)

## Slide 14: Next experiment: Test D injection and measure D content
Chemical Dissolution:
*Hiyane et al, 2016
Thermal desorption spectroscopy
T
Desorption flux
Thermal desorption branch
D2
Measure desorption flux in vacuum with leak detector
Deuterium content
t
Testing of deuterium injection system:
Measuring D concentration in Li samples:
In a next experiment, the Li will be loaded with D.
A lithium sample will be extracted.
The Li will be pumped through trap several times.
Another lithium sample will be extracted.
Alternative 1: Extracted samples will be analyzed on their Li concentration by TDS by plugging the sampler to the TDS branch.
Alternative 2: Samples will be dropped into container and analyzed by the chemical dissolution method.

## Slide 15
EcosimPro model of LYDER lithium branch was created to simulate concentration decrease.
Only ratio of concentrations must be measured!
Measurement of temperatura-dependent
dissociation coefficient KD :
Minimum required Y mass for H-trap during DONES operation if replacement rate 28 days:
S.J. Hendricks et al, Impact of yttrium hydride formation on multi-isotopic hydrogen retention by a getter trap for the DONES lithium loop, Nucl. Fusion 63 (2023) 056012 (27pp), https://doi.org/10.1088/1741-4326/acc31a
S.J. Hendricks et al, Modeling and experimental design to characterize permeation and gettering of hydrogen isotopes in fusion materials, Doctoral Dissertation (2023), https://info.fusion.ciemat.es/PhDThesis/Hendricks.pdf
Future work: Measure Y-Li distribution coefficient KD

## Slide 16: Conclusion and work pending
Conclusion
The LYDER lithium system is fully constructed and the heating and cooling systems successfully commissioned.
The movement of liquid lithium in LYDER could be demonstrated as previsioned in the initial design.
The functioning of the lithium level sensors and the extraction of liquid lithium samples could be demonstrated.
The removal and subsequent installation of the lithium-exposed LYDER D-trap could be demonstrated.
Test of D injection and D concentration measurement pending due to failure of heater and Ar purification system.
Work pending
Test of successful functioning of the LYDER deuterium injection system.
Test of thermal desorption spectroscopy and chemical dissolution method to determine deuterium concentration in extracted lithium samples.
Measure deuterium concentration in lithium samples before and after exposure to the yttrium bed.
Determine distribution coefficient of the Y-Li-D system to obtain min. required Y mass for DONES.
Problems that caused delay of experimental progress
A heating wire has broken and had to be replaced which required opening the glove box and removing and reattaching thermal insulation.
The glovebox purification system failed causing the argon in the box to be contaminated. It is currently waited for the purification system to be repaired which might take one to two months.

## Slide 17: Thank you very much for your attention!

## Slide 18: Appendix

## Slide 19: LYDER - Lithium Yttrium system for DEuterium Retention studies

## Slide 20: Design and manufacturing of homemade glovebox system
Glovebox airlock system for sample insertion:
Glovebox adapted to needs for the LYDER lithium experiment:
160 cm
60 cm
120 cm
Glovebox and antechamber has been designed and manufactured within scope of the PhD!

## Slide 21: LYDER - Lithium Yttrium system for DEuterium Retention studies
Glovebox antechamber
Thermal desorption branch
Electrical feedthrough for heaters
Mounted electrical feedthrough for heating wires

## Slide 22
Chemical Dissolution:
Hiyane et al, 2016
Thermal desorption spectroscopy
Measuring techniques
T
Desorption flux
TDS
D2
Measure desorption flux in vacuum with leak detector
EcosimPro model of LYDER lithium branch created!
Connect
sampler
Deuterium content
t

## Slide 23: Appendix

## Slide 24: Appendix

## Slide 25: Appendix

## Slide 26: Appendix

## Slide 27: Appendix

## Slide 28: Appendix

## Slide 29: Appendix

## Slide 30: Future experiments
EcosimPro model of LYDER lithium branch was created to simulate concentration decrease.
Only ratio of concentrations must be measured!
Measurement of temperatura-dependent
dissociation coefficient KD :
Minimum required Y mass for H-trap during DONES operation if replacement rate 28 days:
S.J. Hendricks et al, Impact of yttrium hydride formation on multi-isotopic hydrogen retention by a getter trap for the DONES lithium loop, Nucl. Fusion 63 (2023) 056012 (27pp), https://doi.org/10.1088/1741-4326/acc31a
S.J. Hendricks et al, Modeling and experimental design to characterize permeation and gettering of hydrogen isotopes in fusion materials, Doctoral Dissertation (2023), https://info.fusion.ciemat.es/PhDThesis/Hendricks.pdf

## Slide 31: Fully mounted LYDER experimental setup
Glove box purification system
Heat exchanger
Water chiller
Antechamber
Pressure control panel
Outlet pipes toward heat exchanger
Lithium system
Vacuum system
LYDER Li system constructed inside of a custom designed argon-filled glove-box fabricated at Ciemat
Glove box