## Slide 1: Experimental methodology and feasibility studies on the characterization of Be solubility in liquid lithium

## Slide 2: SUMMARY
Context
Measurement of Solubility with open Iron Crucible and Capsules
Experimental campaign

## Slide 3: Context (1/2)
Lithium-Beryllium Phase Diagram
A large dispersion in the solubility of Be in liquid lithium was found
The origin of the large differences in solubility can be explained by the experimental conditions and impurities in the lithium.
Beryllium is in different forms Be(Li) and Be3N2 (Li) depending on the nitrogen content, which influences the amount of beryllium dissolved in the solution.
Whether beryllium is present in lithium, in dissolved chemical form, or in particulate form,

## Slide 4: Measurement of Solubility with open Iron Crucible and Capsules (1/3)
Solubility measurement between 180°C and 650°C
Method:
Addition of beryllium, lithium and lithium nitrides to the crucible
Heats the crucible to the desired temperature and maintains the temperature until maximum solubility is reached (Equilibrium Time)
Take representative sample at equilibrium (at the supernatant level) using an iron pipette.
The crucible is then cooled to another target temperature lower than the previous one and maintained until a new equilibrium is reached.
The pipette takes another sample leaving a space between measurements
When all measurements have been completed, the pipette will be cooled to room temperature
Cut out the pipette for measuring the quantity of beryllium and lithium by direct analysis (GDMS)

## Slide 5: Measurement of Solubility with open Iron Crucible and Capsules (2/3)
Solubility measurement between 650°C and 1300°C
Method:
Addition of beryllium, lithium and lithium nitrides to the capsules
Welded iron cover on all capsules
Heats the capsules to the desired temperature and maintains the temperature until maximum solubility is reached (Equilibrium Time)
The capsules containing the samples will be quickly cooled in water or with liquid nitrogen to freeze the dissolved beryllium in lithium.
Cut out the capsules for measuring the quantity of beryllium and lithium by direct analysis (GDMS)

## Slide 6: Measurement of Solubility with open Iron Crucible and Capsules (3/3)
Analyses by GDMS
The method used to know the amount of beryllium in the sample will be a GDMS (Glow Discharge Mass Spectrometry) analysis method.
This method will be able to experience with an accuracy up to 0.05 ppm (20% uncertainty). It is necessary to provide to the analysis laboratory that will carry out these measurements different lithium cylinder with 2 cm in diameter and 3 cm thick.
For this reason, the inner diameter of the capsule and pipette is 2 cm.
Solubility measurement between 180 and 650°C
Solubility measurement between 650 and 1300°C

## Slide 7: Experimental campaign (1/2)
Various preliminary tests must be carried out before solubility measurements:
Measure the corrosion of the mixture of lithium, beryllium and lithium nitrides in the iron crucible on the surface condition to size the crucible
Define equilibrium time by measuring solubility at defined times

## Slide 8: Experimental campaign (2/2)
 | 0ppm | 10ppm | 30ppm | 40ppm | 50ppm | 750°C | 850°C | 950°C
experience 1 | X |  |  |  |  | X |  | 
experience 2 |  | X |  |  |  | X |  | 
experience 3 |  |  | X |  |  | X |  | 
experience 4 |  |  |  | X |  | X |  | 
experience 5 |  |  |  |  | X | X |  | 
experience 6 | X |  |  |  |  |  | X | 
experience 7 |  | X |  |  |  |  | X | 
experience 8 |  |  | X |  |  |  | X | 
experience 9 |  |  |  | X |  |  | X | 
experience 10 |  |  |  |  | X |  | X | 
experience 11 | X |  |  |  |  |  |  | X
experience 12 |  | X |  |  |  |  |  | X
experience 13 |  |  | X |  |  |  |  | X
experience 14 |  |  |  | X |  |  |  | X
experience 15 |  |  |  |  | X |  |  | X
 | 0ppm | 10ppm | 30ppm | 40ppm | 50ppm | 180°C | 250°C | 350°C | 400°C | 550°C
experience 16 | X |  |  |  |  | X | X | X | X | X
experience 17 |  | X |  |  |  | X | X | X | X | X
experience 18 |  |  | X |  |  | X | X | X | X | X
experience 19 |  |  |  | X |  | X | X | X | X | X
experience 20 |  |  |  |  | X | X | X | X | X | X
In the first campaign of experiments, 20 experiments will be carried out and will make it possible to obtain 40 solubility values as a function of temperature and nitrogen concentration.
Each experiment from 1 to 15 will be in single capsules with nitrogen contents and temperature indicated in Table 1.
Each experiment from 16 to 20 will be carried out in the crucible with several temperatures indicated in Table 2.
In experiments using the capsule method, all experiments with the same temperature will be carried out at the same time, which is 5 capsules in same time.
Table 1 : Description of experimental campaign with capsules method (ppm of nitrogen and temperature)
Table 2 : Description of experimental campaign with crucible method (ppm of nitrogen and temperature)

## Slide 9: Thank you for your attention