## Slide 1: Detailed irradiation parameters assessment of the IFMIF-DONES HFTM irradiation capsules
I. Álvarez, M. Anguiano, F. Mota, R. Hernández, Y. Qiu, F. Arbeiter, J. Park

## Slide 2: Introduction
Test Cell
IFMIF-DONES

## Slide 3: High Flux Test Module
Test Cell
HFTM
469.1 mm
106 mm
32 RIG

## Slide 4: Considerations
The neutron fluence rate is very different from one capsule to another and also within the same capsule
Objective of this work: estimate dose uncertainties in specimen evaluation
To study how the specimens distribution influences the dose and its uncertainty
To study the different configurations available for the rigs, analysing the neutron fluence rate, the NRT_dpa and the gas production

## Slide 5: STACK MODELS
Characteristics of specimen distribution |  |  | 
 | Homogeneous | CLC.v1.0 | CLC.v2.0
Eurofer volume [%] | 75 | 48.16 | 84.76
Liquid metal (Na) [%] | 25 | 21.86 | 12.92
Specimens per rig | Not defined | 101 | 120

## Slide 6
IFMIF-DONES TC MCNP model version used: mdl9.2.0 (2020) and mdl9.2.8 (2023), KIT/INR
McDelicious 2017
Nuclear Data libraries used:
  FENDL3.1d nuclear data libraries for neutron transport calculations
  JEFF3.3DPAarc nuclear data libraries for primary displacement damage calculations in eurofer. (26001.32y)
The statistic relative error has been lower than 0.05 for all bins.
Deuteron IFMIF-EVEDA E= 40 MeV, 125 mA, footprint size 20x5 and 10x5 cm²
Full power year (fpy) = 365.25 days
Volume has been obtained by meshtal for HFTM and tallies for specimens cells
Methodology
Notes: For particle transport we have used, the McDelicious code, based on MCNP, and the latest version of the test cell. Here we indicate the libraries used. He have obtained data for two deuteron beam size: 20x5, 10x5

## Slide 7: Primary displacement damage rate
Volume DPA requirements [L] |  |  | Results [L] | 
 |  | Target value | Homogeneous/CLC.v1.0/CLC.v2.0 | 
 | Beam |  | 10x5 | 20x5
R-1 | 8-12 NRT_dpa/fpy | 0.3 | 0.2 | 0.3
R-2 | >16.7 NRT_dpa/fpy | 0.1 | 0.2 | 0.1
Integrated HFTM volumen in specimens region

## Slide 8: Primary displacement damage rate
Eurofer | 
Box, filling objects | Specimens
Integrated stack and specimens in HFTM volumen

## Slide 9: Primary displacement damage rate
Units/rig |  |  | 
 | Type | CLC.v1.0 | CLC.v2.0
Tensile |  | 52 | 64
FCG |  | 17 | 22
Fatigue |  | 9 | 9
FT |  | 11 | 13
KLST |  | 12 | 12
Primary displacement damage rate [NRT_dpa/fpy]
DPA variation by specimen type in 20x5 cm² beam footprint
CLC.v2.0 model
CLC.v1.0 model
Volume [cm³]
No. of specimens

## Slide 10: Gas –production

## Slide 11: Neutron fluence rate [n/cm²s­]
1∙10¹³
2∙10¹³
5∙10¹³
1∙10¹⁴
2∙10¹⁴
5∙10¹⁴
BEAM
CLC.v2.0 model
CLC.v1.0 model
2 ∙10¹⁴
5 ∙10¹⁴
1 ∙10¹⁴
5∙10¹³
2∙10¹³
2 ∙10¹⁴
5 ∙10¹⁴
1 ∙10¹⁴
5∙10¹³
2∙10¹³

## Slide 12: Neutron fluence rate [n/cm²s­]
1∙10¹³
2∙10¹³
5∙10¹³
1∙10¹⁴
2∙10¹⁴
5∙10¹⁴
BEAM
CLC.v2.0 model
CLC.v1.0 model
RIG 43
RIG 43
RIG 26
RIG 26
Self Powered Neutron Detector
(SPND)

## Slide 13: Neutron fluence rate
Neutron fluence rate 20x5 cm² beam footprint [10¹⁴ n/cm²s] |  |  |  |  |  |  |  | 
Model | CLC.v1.0 |  |  |  | CLC.v2.0 |  |  | 
RIG | 43 |  | 26 |  | 43 |  | 26 | 
Layout |  |  |  |  |  |  |  | 
Min | 1.58 | -44.8% | 0.76 | -29.5% | 1.77 | -42.7% | 0.78 | -30.9%
Max | 4.54 | 58.7% | 1.60 | 48.1% | 4.84 | 56.6% | 1.50 | 38.9%
Average | 3.12 | 9.1% | 1.16 | 7.4% | 3.23 | 4.5% | 1.15 | 1.8%
SPND | 2.86 |  | 1.08 |  | 3.09 |  | 1.13 | 
1∙10¹³
2∙10¹³
5∙10¹³
1∙10¹⁴
2∙10¹⁴
5∙10¹⁴

## Slide 14: Neutron fluence rate
Neutron fluence rate 20x5 cm² beam footprint [10¹⁴ n/cm²s] |  |  |  |  |  |  |  | 
Model | CLC.v1.0 |  |  |  | CLC.v2.0 |  |  | 
RIG | 43 |  | 26 |  | 43 |  | 26 | 
Layout |  |  |  |  |  |  |  | 
Min | 1.58 | -44.8% | 0.76 | -29.5% | 1.77 | -42.7% | 0.78 | -30.9%
Max | 4.54 | 58.7% | 1.60 | 48.1% | 4.84 | 56.6% | 1.50 | 38.9%
Average | 3.12 | 9.1% | 1.16 | 7.4% | 3.23 | 4.5% | 1.15 | 1.8%
SPND | 2.86 |  | 1.08 |  | 3.09 |  | 1.13 | 
1∙10¹³
2∙10¹³
5∙10¹³
1∙10¹⁴
2∙10¹⁴
5∙10¹⁴

## Slide 15: Primary displacement damage rate
25 MeV
30 MeV
35 MeV
40 MeV
25 MeV
30 MeV
35 MeV
40 MeV
Primary displacement damage rate [NRT_dpa/fpy]
Different deuterom beam energy for the CLC.v2.0 model HFTM volume
IFMIF-EVEDA 20x5 cm² BEAM
IFMIF-EVEDA 10x5 cm² BEAM

## Slide 16: Gas-production
35 MeV
40 MeV
25 MeV
30 MeV
10x5 cm² Beam
IFMIF-EVEDA BEAM
20x5 cm² Beam
35 MeV
40 MeV
25 MeV
30 MeV
35 MeV
40 MeV
25 MeV
30 MeV
35 MeV
40 MeV
25 MeV
30 MeV
H Ratio [H app/dpa]
He Ratio [H app/dpa]
Different deuterom beam energy for the CLC.v2.0 model

## Slide 17: Conclusions
Considering the whole volume of the HFTM, R-1 and R-2 criteria of dpa are fulfilled

## Slide 18: Conclusions
Considering the whole volume of the HFTM, R-1 and R-2 criteria of dpa are fulfilled
NRT_dpa histograms by specimen type show the versatility of this facility, because depending on the specimens distribution design, it is possible to obtain different values. The gradient inside a rig must be also considered

## Slide 19: Conclusions
Considering the whole volume of the HFTM, R-1 and R-2 criteria of dpa are fulfilled
NRT_dpa histograms by specimen type show the versatility of this facility, because depending on the specimens distribution design, it is possible to obtain different values. The gradient inside a rig must be also considered
The gas production ratios cover the expected values for DEMO

## Slide 20: Conclusions
Considering the whole volume of the HFTM, R-1 and R-2 criteria of dpa are fulfilled
NRT_dpa histograms by specimen type show the versatility of this facility, because depending on the specimens distribution design, it is possible to obtain different values. The gradient inside a rig must be also considered
The gas production ratios cover the expected values for DEMO
By changing the beam energy, the desired dpa ranges can be changed, as well as the gas production

## Slide 21: Future work
Results will be obtained for different materials such as W or CuCrZ
The isotopic composition of these materials and eurofer will be obtained, because they will also affect the macroscopic properties of the material
Estimation the signal in the SPND and activation foils
Thank you very much for your attention
Irene Álvarez Castro (iac@ugr.es)
PhD Student
Department of Atomic, Molecular and Nuclear Physics
University of Granada