## Slide 1: Solid Breeding Blankets: overview and key pending validation needs
Guangming Zhou, Francisco A. Hernández, Arkady Serikov (KIT)
Alessandro Spagnuolo, Salvatore D’Amico (EUROfusion DEMO Central Team)

## Slide 2: Outline of content
Solid breeding blankets in Europe: Overview
  Helium Cooled Pebble Bed (HCPB)
  Water cooled Lead and Ceramic Breeder (WLCB)
Key pending validation needs

## Slide 3: Solid breeding blanket in Europe: HCPB – Helium Cooled Pebble Bed
    ↑↑ Robustness (in-box LOCA)
    ↓↓ TBR (1.06)
    ↑↑ Fabrication & assembly complexity
    ↑↑ ∆p (Ppump≈250MW, low TRL BoP)
    ↑ Robustness (in-box LOCA)
    ↑ TBR (1.15)
    ↑ Fabrication & assembly complexity
    ↑ ∆p (Ppump≈150MW, low TRL BoP)
    ↑ Robustness (in-box LOCA)
    ↑ TBR (1.20)
    ↓ Fabrication & assembly complexity
    ↓ ∆p (Ppump≈ 90MW, high TRL BoP)
    Low reliability, low availibility of DEMO
    PPCS Model B (HCPB)
    ITER HCPB TBM „act-alike“
    DEMO baseline 2014
    DEMO baseline 2015
    DEMO baseline 2017
2014
2015
2016
2017
2018
2019
2020
HCPB and WCLL are two driver blanket concepts for EU DEMO
2021
2022
2023
Concept Design Phase (FP9)
Pre-Concept Design Phase (FP8)
    ↑ Robustness (in-box LOCA)
    ↑ TBR (1.20)
    ↓ Fabrication & assembly complexity
    ↓ ∆p (Ppump≈ 90MW, high TRL BoP)
    ↑ High reliability
G. Zhou et al. 2022. TOFE 2022
G. Zhou et al. 2023. ISFNT-15
80 bar
2 bar
2 bar
2 bar
80 bar
80 bar
80 bar
80 bar
80 bar
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 3/15
  Coolant: He @80 bar, 300-520°C
  T-breeder: Li-ceramic pebbles
  n-multiplier: Beryllide
  T-extraction: purge gas
  Structural steel: Eurofer97
''Beer-box''
''Sandwich''
''Fuel-breeder pin''
Hernández FA et al., 2020 Fusion Eng Des 157, 111614.
Li-ceramic pebble
Beryllide block

## Slide 4: Solid breeding blanket in Europe: HCPB high pressure purge gas
  Coolant: He @80 bar, 300-520°C
  Structural steel: Eurofer97
  Fuel-breeder pins contain advanced ceramic breeder (ACB) pebble
  Beryllide neutron multiplier of triangular prism with lateral edges filleted
  T-extraction: He + 200 Pa H2 @80 bar
  FW and critical structure thicker + cooler by fresh coolant
  Inner beryllide block inside ACB pebble
  Nuclear, thermal hydr. & thermal-mech. analysis confirmed soundness
HCPB-BL2017-HP-v1
Shield
FW
Armor
TiBe12 outer block
TiBe12 inner block
ACB pebbles
Detail A: Fuel-breeder pin
Pressure tube
Closing disk
80 bar
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 4/15

## Slide 5: Exploring variant: WLCB – Water coold Lead and Ceramic Breeder
  Seen as a best trade-off between HCPB and WCLL:
    To avoid current issues in HCPB with shielding, multiplier technology and costs
    To mitigate issues with T-permeation and avoid T-extraction risks from PbLi in WCLL
    To avoid use of anti-permeation barriers in BB
    To use proven water PWR tech.
WLCB
HCPB
WCLL
Proven water PWR tech
Excellent neutron shielding
More mature PHTS/BoP
T extraction from ACB
Low T permeation (no need for T barriers)
Available TER technology
Good TBR in compact space
  Background:
    Idea started in FP8: HCPB issue with beryllium -> deep exploration of alternative n-multipliers -> Pb/Pb-alloy
    He-cooled molten lead and ceramic breeder blanket
    Curiosity for a water cooled version -> WLCB, as radial fuel-breeder pins
Hernández FA et al. 2023, ISFNT-15
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 5/15
Zhou G et al. 2021, Fusion Eng Des 168: 112397
Hernández FA et al. 2019, Fusion Eng Des 146:1186–1191
Zhou G et al. 2019, Fusion Eng Des 146:1029–1034
HCPB: Helium Cooled Pebble Bed
WLCB: Water cooled Lead and Ceramic Breeder
WCLL: Water Cooled Lithium Lead

## Slide 6: Exploring variant: WLCB Design evolution
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 6/15
Zhou G et al. 2021, Fusion Eng Des 168: 112397.
2019-2020
2021-2023
Hernández FA et al. 2023, ISFNT-15
Pre-Concept Design Phase (FP8)
Concept Design Phase (FP9)
2023-
Feasibility study of a WLCB based on the fuel-breeder pin architecture, in terms of T-breeding, temperature and stress limits.
Too many welds, low reliability, low availiability
High reliability
Tritium breeding and T-permeation
Second pass, T extraction
First pass, advection
Cooling plates
ACB pebbles in tubes
Molten Pb pool

## Slide 7: Challenging environment in fusion power plant
High dose rate
High pressure (80 bar for HCPB, 155 bar for WLCB)
High temperature gradient
Displacement per atom accumulation in the BB structure
Temp. [°C]
3 mm
80 bar
Temp. on FW
Neutron flux at breeding zone
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 7/15

## Slide 8: Challenges and pending validation needs of HCPB & WLCB
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 8/15
w/o neutrons
w/ neutrons
Fusion environment
  Changes in properties and behaviour of materials
    Effect of heat flux and cycling on fatigue or crack growth-related failure
    Premature failure at welds
    Effect of swelling, creep and thermal gradients on stress
  Tritium permeation through the structure
    Tritium permeation through structure into coolant
    Effect of radiation on tritium permeation
  Structural activation product inventory
  Blanket supporting structure to Vacuum Vessel
  Failure modes & rates of blanket structure under fusion environ.
Structure
  Mechanical and materials interactions
    Corrosion
    Failure of coolant wall due to stress corrosion cracking
    Failure of coolant wall due to liquid-metal embrittlement
  Neutron-induced sputtering transp. of activated mat.
  Coolant/coatings/structure interactions
Coolant / structure interactions
  Tritium release, recovery and inventory in solid breeder and multiplier
  Thermal conduct. changes of Breeder and Multiplier under irradiation
  Tritium transport in blanket system
  Breeder behaviour under high dpa
  Solid multiplier behaviour under high dpa
Breeder/multiplier and purge
  Uncertainties in required T breeding ratio
  Uncertainties in achievable T breeding ratio
  Tritium trapping
  Tritium permeation to blanket coolant
  Failure modes and rates
  Nuclear heating rate predictions
  Prediction and control of radioactive effluent
General for all concepts
Abdou MA et al. 1985, Fusion Technology 8:3, 2595-2645
Spagnuolo A et al., this session
Tungsten and EUROFER qualification & design code not included here, dealt in WPMAT.
  Solid breeder mechanical and materials interactions
    Pebble-steel interaction under purge gas environment
    Load on wall induced by Pebble expansion/swelling
    Dust formation and transport of pebble bed
  Neutron multiplier mechanical interactions
    Beryllide swelling and interact with wall
    Cracking of Beryllide block due to thermal stress
    Compatibility of neutron multiplier and Li-ceramics
  Thermal interactions
    Breeder/multiplier-structure heat transfer (gap conductance)
Solid Breeder / multiplier / structure interactions

## Slide 9: Ongoing activities
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 9/15
w/o neutrons
w/ neutrons
Fusion environment
  Changes in properties and behaviour of materials
    Effect of heat flux and cycling on fatigue or crack growth-related failure
    Premature failure at welds
    Effect of swelling, creep and thermal gradients on stress
  Tritium permeation through the structure
    Tritium permeation through structure into coolant
    Effect of radiation on tritium permeation
  Structural activation product inventory
  Blanket supporting structure to Vacuum Vessel
  Failure modes & rates of blanket structure under fusion environ.
Structure
Thermomechanic cycling of FW at HELOKA
Tritium permeation cell at Tritium Laboratory Karlsruhe
Remote Handling Test Facility
Kohpeiss J et al., 2023, Fusion Science and Technology
Zhou G et al., 2021, EUROfusion report
Crofts O. 2023, ISFNT-15

## Slide 10: Ongoing activities
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 10/15
w/o neutrons
w/ neutrons
Fusion environment
  Mechanical and materials interactions
    Corrosion
    Failure of coolant wall due to stress corrosion cracking
    Failure of coolant wall due to liquid-metal embrittlement
  Neutron-induced sputtering transp. of activated mat.
  Coolant/coatings/structure interactions und irrad.
Coolant / structure interactions
WLCB
learn from fission

## Slide 11: Ongoing activities
w/o neutrons
w/ neutrons
Fusion environment
  Tritium release, recovery and inventory in solid breeder and multiplier
  Thermal conduct. changes of Breeder and Multiplier under irradiation
  Tritium transport in blanket system
  Breeder behaviour under high dpa
  Solid multiplier behaviour under high dpa
Breeder/multiplier and purge
Irradiation campaigns at BR2, Belgium and WWR-K, Kazakhstan
Kulsartov T et al., 2022, Nucl. Mat. Energ., 30:101115
Tritium Release Test Module in IFMIF/DONES
Abou-Sena A, Arbeiter F. 2013, Fusion Eng. Des. 88: 818-823
Arbeiter F, this session
Limited irradiation space
Φ22 mm in WWR-K
400 x 400 x 950 mm³
Space for breeder/multiplier
400
400
950
Unit: mm
345 mm
Qiu Y. 2023, private communication
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 11/15

## Slide 12: Ongoing activities
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 12/15
w/o neutrons
w/ neutrons
Fusion environment
  Solid breeder mechanical and materials interactions
    Pebble-steel interaction under purge gas environment
    Load on wall induced by Pebble expansion/swelling
    Dust formation and transport of pebble bed
  Neutron multiplier mechanical interactions
    Beryllide swelling and interact with wall
    Cracking of Beryllide block due to thermal stress
    Compatibility of neutron multiplier and Li-ceramics
  Thermal interactions
    Breeder/multiplier-structure heat transfer (gap conductance)
Solid Breeder / multiplier / structure interactions
Pebble Bed Test Module in DONES?
After 200 cycles
Thermal cycling using induction heating at Ulba/KIT
Gaisin R et al., 2022, 15th International Workshop on Beryllium Technology
Solid Neutron Multiplier Test Module in DONES?
Ageing of Eurofer97 in contact with pebbles under purge gas environment, 550°C, HELOKA-HEMAT
Krüssmann R et al., 2023, ISFNT-15

## Slide 13: Challenges and pending validation needs of HCPB & WLCB
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 13/15
w/o neutrons
w/ neutrons
Fusion environment
  Solid breeder mechanical and materials interactions
    Pebble-steel interaction under purge gas environment
    Load on wall induced by Pebble expansion/swelling
    Dust formation and transport of pebble bed
  Neutron multiplier mechanical interactions
    Beryllide swelling and interact with wall
    Cracking of Beryllide block due to thermal stress
    Compatibility of neutron multiplier and Li-ceramics
  Thermal interactions
    Breeder/multiplier-structure heat transfer (gap conductance)
Solid Breeder / multiplier / structure interactions
Solid Neutron Multiplier Test Module in DONES?
Pebble Bed Test Module in DONES?
Blanket Functional Materials Module
in DONES?
A-A view
A-A
DONES Test Cell
Fuel-breeder pin
of HCPB

## Slide 14: Challenges and pending validation needs of HCPB & WLCB
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 14/15
w/o neutrons
w/ neutrons
Fusion environment
  Uncertainties in required T breeding ratio
  Uncertainties in achievable T breeding ratio
  Tritium trapping
  Tritium permeation to blanket coolant
  Failure modes and rates
  Nuclear heating rate predictions
  Prediction and control of radioactive effluent
General for all concepts
Fusion neutrons
with sufficient space for qualifying blankets

## Slide 15: Conclusions
Guangming Zhou et al. | 2nd DONES Users Workshop | 19.10.2023 | 15/15
w/o neutrons
w/ neutrons
Fusion environment
  Changes in properties and behaviour of materials
    Effect of heat flux and cycling on fatigue or crack growth-related failure
    Premature failure at welds
    Effect of swelling, creep and thermal gradients on stress
  Tritium permeation through the structure
    Tritium permeation into coolant
    Effect of radiation on tritium permeation
  Structural activation product inventory
  Blanket supporting structure to Vacuum Vessel
  Failure modes & rates of blanket structure under fusion environ.
Structure
  Solid breeder mechanical and materials interactions
    Pebble-steel interaction under purge gas environment
    Load on wall induced by Pebble expansion/swelling
    Dust formation and transport of pebble bed
  Neutron multiplier mechanical interactions
    Beryllide swelling and interact with wall
    Cracking of Beryllide block due to thermal stress
    Compatibility of neutron multiplier and Li-ceramics
  Thermal interactions
    Breeder/multiplier-structure heat transfer (gap conductance)
Solid Breeder / multiplier / structure interactions
  Mechanical and materials interactions
    Corrosion
    Failure of coolant wall due to stress corrosion cracking
    Failure of coolant wall due to liquid-metal embrittlement
  Neutron-induced sputtering transp. of activated mat.
  Coolant/coatings/structure interactions
Coolant / structure interactions
  Tritium release, recovery and inventory in solid breeder and multiplier
  Thermal conduct. changes of Breeder and Multiplier under irradiation
  Tritium transport in blanket system
  Breeder behaviour under high dpa
  Solid multiplier behaviour under high dpa
Breeder/multiplier and purge
  Uncertainties in required T breeding ratio
  Uncertainties in achievable T breeding ratio
  Tritium trapping
  Tritium permeation to blanket coolant
  Failure modes and rates
  Nuclear heating rate predictions
  Prediction and control of radioactive effluent
General for all concepts
Out-of-pile and in-pile tests in MTRs for basic tests
DONES could offer unique test platform for irrad. function. mat.
Fusion neutron source is needed for blanket qualification

## Slide 16: Backup slides: Nuclear responses of HCPB BB
DPA of E97
DPA of TiBe12 and Li-pebble
T-generation
Power density
Neutron flux at breeding zone at contral IB
Burn-up/fpy
5
16
Zhou G et al., 2023, HCPB Design and Analysis Report

## Slide 17: Backup slides
Investigating the evolving behavior of the pebble bed and beryllide neutron multiplier together, for example, it can be that the breeder undergoes chemical processes (due to burn-up and due to contact to other material), the pebble bed can change its thermal conductivity and consequently shift the temperature field which is decisive for the tritium release residence times
The pebbles will mechanically deform and it will be interesting to study their interacting within the bed and also with the walls
Dust formation and transport of pebble bed in the purge gas flow path
Measuring the time structure of tritium release from this complex setup with broad temperature spread and realistic (not 1-D) purge flow path (as opposed to the well-defined "academic type" TRTM)
A specific question concerns the cracking/blistering of the berillyde block, which is larger than a TRTM capsule
17