## Slide 1
Tritium Release Test Module - design overview
Frederik Arbeiter (KIT), A. Abou-Sena (KIT), Y. Qiu (KIT), A. Valentine (UKAEA), H. Chohan (UKAEA) Second DONES User Workshop, 19.–20. Oct. 2023, Granada, Spain.
DONES Preparatory Phase

## Slide 2: Scope of reported work on “TRTM”
IFMIF/EVEDA 2011-2013 “Tritium Release Test Module” KIT , “DDD-III”
  Conceptional design
  Neutronics, thermal, mechanical, tritium transport analyses
  Purge system, tritium analysis station
  CAD model + production drawings (capsule prototype parts fabricated)
DONES-PreP 2019-2021“In-Situ Ceramic Breeder Irradation Module” KIT, UKAEA, “Del.8.3.2” + attached ICBIM DDD
  Update and detailing of neutronics (DONES specific)
  Update of test requirements

## Slide 3: TRTM mission statement
The TRTM is the device dedicated for
  irradiation of breeder ceramics or solid neutron multiplier materials,
  at controlled temperatures ( 300 – 1100 °C ) in bounded intervals,
  in the high/medium flux region of the DONES neutron source,
  for long term periods (months),
  with the ability to monitor on-line the release of tritium species to a purge flow,
  with the ability to retrieve the irradiated materials for PIE.

## Slide 4: Specific test objectives [DONES-PreP Del8.3.2]
1. Determination of time structure (so called residence time) of tritium release from Li ceramics, as reaction to transients {n-flux, temperature, purge gas} and as function of age.
2. Determination of chemistry of the purge gas and tritium / hydrogen species, i.e. fractions of HT, HTO etc. during irradiation
3. Determination of change of mechanical properties {dimensional stability, microstructural evolution, crushing load} - and physical properties {thermophysical properties, density, tritium diffusivity} by PIE

## Slide 5: Some underlying physics questions
Transport mechanisms of tritium from “place of birth” into purge gas flow
Evolution of properties driven by progressing transmutation (Li-burnup), radiation damage and chemistry
[Raffray, Abdou, Federici]
Can only be studied with real breeding Li(n,T), otherwise T-source in volume can be achieved !
Tritium release rate determines the reactors T-inventory /safety !
[Scaffidi-Argentina, Werle]
10%
OSi pebbles EXOTIC-7
Li burnup:
10%
13%
18%
18%
Thermal desorption tests

## Slide 6: Example irradiation conditions (DEMO HCPB 2021)
Breeder material: KALOS-ACB pebbles : Li4SiO4 with 30 mol-% of Li2TiO3
Polydisperse pebble bed 250 – 1250 µm (typical diameter 625 µm), packing fraction 63-64%
Purge gas: helium with 0.1-wt% of H2 at 0.2 MPa abs. (Changed to 8MPa!), superficial velocity 29 to 46.3 mm/s
Temperatures in the pebble bed are predicted at
  320 - 360°C minimum, given by the coolant helium outlet temperature from the FW
  around 600 - 800 °C in large bulk regions
  1055 °C peak
Neutron flux in BZ : 5×1013 to 7×1014 n/cm²/s
Tritium production : 0.5 – 1.7 ×1019 atoms(T)/m3/s in the breeder material
Volumetric heating in BZ : 4 – 20 W/cm³

## Slide 7: TRTM mode of operation
Loading capsules with unirradiated specimen material
Inserting TRTM into DONES TC
During irradiation:
  Controlled setpoint changes {Temperature, purge gas, neutron flux} OR: observe long-term changes
  Registering time dependent {T-activity, Temperature, purge flow conditions etc.}
Retrieve TRTM, Extract specimens
Perform PIE on irradiated specimens {microstructure, mechanical, T-desorption}
Simplified P&ID of TRTM in DONES
n-flux
T-activity
time
Example of transient
measurements with TRTM

## Slide 8: Design challenges (1) : Temperature management
Achieve high temperatures as in BZ (1100 °C)
  Electrical heater limits 600 – 1000 °C, worse under irradiation (RIC, RIED)
  Mechanical limits of materials (creep etc.)
Limit temperature spread within specimen region
Inner cylinder “specimen bin” contains specimens, high-temp. alloy, no pressure-diff. effective
Two concentric gaps (stagnant gas) achieve thermal isolation, Theater < Tspecimens
Pressure bearing wall and final tritium diffusuion barrier “rig hull” is cold
Temperature difference within specimen stack is limited so that diffusivity varies by max. 10%
specimen
inner gap
outer gap
“heater can”
specimen capsule
rig hull
coolant
Maximum temperature achieved (by analysis) ~ 900 °C
radius
temperature
heater

## Slide 9: Design challenges (2) : tritium containment
Without recovery, 94% of bred T reaches the analysis station (losses over hot capsule wall)
“Periodic sweeping” can be implemented by oscillating the purge gas pressure (part of the 6% losses are recovered)
Losses from rig are < 10-4 “of production
Loss f. capsule
Production
Loss f. rig
T-fluxes

## Slide 10: TRTM configuration
185mm
Container: 316L(N) stainless steel
Nuclear grade graphite
Mass ~350 kg + interface head

## Slide 11: TRTM capsule
Specimen capsule made of High-Cr stainless steel X15CrNiSi25-21
Specimen volume D=19mm L=86mm 33 cm³
3 Thermocouples
Thermocoax heater (Inconel)
ID 4 mm purge tubes
86 mm

## Slide 12: Nuclear analyses
Li-Target
W-Spectrum
Shifter
TRTM
9.0 ×1017 T-atoms/m³/s
1.20 W/cm³
7.9 ×1017 T-atoms/m³/s
1.05 W/cm³
3.9 ×1017 T-atoms/m³/s
0.45 W/cm³
HCPB DEMO BZ:
5×1013 to 7×1014 n/cm²/s
0.5 – 1.7 ×1019 T-atoms/m3/s
4 – 20 W/cm³
Neutron flux comparable to DEMO
T-production rate and heating about 1 order of magnitude < DEMO
Further optimization of neutron spectrum advisable (higher flux in low energy range required for Li-6 breeding)
Nuclear analyses completed with activation, decay-heat and dose-rates after shutdown

## Slide 13: Purge gas system, tritium measurements
Antagonistic effect detection rate vs. time resolution as function of flow rate
Expected residence times in pebbles : O(hours)
Detectors: Ionisation Chambers (IC), Liquid scintillation counting, Beta induced X-Ray spectrometry (BIXS)
Typical detector properties: Volume 1 – 3 L Resolution 37 - 37×103 Bq/m³ Range 2×106 - 8×1014 Bq/m³
Purge gas
supply
Feed pipe
TRTM capsule (33cm³)
Return pipe
Detector
system
0.2 MPa
900 °C US=47 mm/s
t=0.7s
5.5×104 Bq/s
L=50m DI=4mm
1 mg/s He
0.25 mmol(He)/s
336 sccm
t=206s, 0.24 m/s
0.15 MPa
20 °C V=1L t=246s 1.36×1010 Bq/m³
DR=1.36×107 Bq
xT=0.14 ppm

## Slide 14: Conclusions
Functions, requirements, mode of operation defined to 2021 HCPB needs
The TRTM is in an advanced conceptual status:
  CAD design + production drawings
  Neutronic, thermal, mechanical, tritium transport analyses
Design promises temperature range up to 900°C, requirements go up to 1100°C
Neutron spectrum could be improved to match DEMO T breeding rate, use of carbon reflectors
Effective tritium containment concept acc. to analyses
Achievable Purge gas- and Tritium measurement parameters (purge gas velocity, activity resolution, time resolution) are compatible with mission

## Slide 15: R&D needs up to deployment
Interfaces definitions vs. DONES plant
Optimization on neutron flux / spectrum DEMO by NSS and NR
Detailed development of purge gas analytics
Improvement of high-temperature capability
Development of RH-compatible interface head vs. Test Cell
Transient temperature steps analyses / control strategy
Detailed material grades selection and fabrication planning
Prototype fabrication (from capsule to module)
Thermal-hydraulic validation (both: coolant & purge loops)
Long-term (lifetime) test of heater at high temperatures
WPENS
‘24+’25

## Slide 16: Fabricated TRTM capsule items

## Slide 17: Limitation of temperature spread